- Firm having Sulphuric Acid based Anodizing Plant with Black Dyeing & Water Sealing facilities are only eligible.

- Firm should have facilities for the Anodizing of the Aluminum Alloys components by sulphuric acid process followed by Black Dyeing & Water Sealing as per technical specification no. 301065774

- ESSENTIAL FACILITIES:

Firm should have: Anodizing plant for producing uniform anodic coating on aluminum alloy surface with following essential facilities :

- Titanium Aluminum jigging & holding arrangement for components

- Pretreatment facility such as Degreasing, Eitching, Rinsing etc

- Sulphuric Acid Anodizing with suitable Rectifiers, chilling system & air agitation

- Non fade black dyeing & water sealing facility

- Temperature indicators / controllers for essential process baths

- Suitable coating thickness meter for measuring anodic coating thickness of 10 microns and above with fine accuracy.

- DESIRABLE FACILITIES:

- De-mineralized water Facility for anodizing plant

- Salt Spray Test facility to specification ISO 9227 or capable to do this test at other suitable laboratory.

- Trained electroplater/ anodizers /suitable competent workmen for carrying out anodizing operation

- Other Standard Terms & Conditions applicable:

- All the required facilities should be capable for anodizing as per dimensional and quality requirement projected in Monitoring Instructions, drawings/specifications. Firm must confirm the same against Technical Bid with self-declaration for capability of firm.

Firm has to arrange for suitable packaging of components to protect the damage during storage and transit if firm gets the order. Firm must confirm the same in Technical Bid.