Structural alloy steel bars

Technical Specifications

GOST 4543 – 71

# Translated by:

M/s SWYAZ

2/453, Viram Khand, Gomti Nagar

# Lucknow – 226016

(: 0522–3098139 / 2345145									Visit us:

http\\:www.swyaz.com

Group B32

state standard of ussr

Structural alloy steel bars

Technical specifications

### OKП 09 5040

Effective period from : 01.01.73

## Non – observance of standard is dealt as per rules

This standard pertains to hot rolled, forged bar of structural alloy steels with diameter or thickness upto 250 mm, calibrated and with special surface finish, to be used in heat treated conditions.

As far as norms of chemical composition, the standard pertains to all the other types of rolled stocks, ingots, forgings and stampings.

(Amended edition, Amendment No. 1, 2, 4, 5)

1. CLASSIFICATION

1.1 Depending upon the chemical composition and properties, structural steel is divided into following categories:

Quality;

High quality  - A;

Very high quality  - Ш.

Note: -

1. The steel of electro slag re-melting belongs to very high quality steel.

2. (Deleted, Amendment No. 2)

1.2 Depending upon the main alloying elements, steel is divided into following groups:

Chromium, manganese, chromium-manganese, chromium-silicon, chromium-molybdenum, chromium-molybdenum-vanadium, chromium-vanadium, nickel-molybdenum, chromium-nickel and chromium-nickel with boron, chromium-silicon-manganese, and chromium-silicon-manganese-nickel, chromium-manganese-nickel and chromium-manganese-nickel with titanium and boron, chromium-nickel-molybdenum,

Chromium-nickel-molybdenum-vanadium and chromium-nickel-vanadium, chromium-aluminium and chromium-aluminium with molybdenum, chromium-manganese-nickel with molybdenum, chromium-manganese-nickel with molybdenum and titanium.

(Amended addition, Amendment No. 3)

1.3	As per the types of processing, the rolled stock is divided as follows:

hot rolled and forged (including with turned or roughened surfaces):

calibrated;

with special surface finish.

  - Depending upon the surface quality, the hot rolled and forged stock is divided into following groups: 1, 2, 3

  - According to condition of materials, rolled stock is manufactured:

without heat treatment;

heat treatment  - T;

cold worked - H (for calibrated and with special surface finish of rolled stock).

1.3 – 1.5. (Amended edition, Amendment No. 5).

2a. Assortment

2a.1. Assortment of rolled stock should correspond to the requirements of GOST 2591 – 88, GOST 2590 – 88, GOST 2879 – 88, GOST 103 – 76, GOST 1133 – 71, GOST 7417 – 75, GOST 8559 – 75; GOST 8560 – 78, GOST 14955 – 77 and other standard technical documents.

(Amended edition, Amendment No. 5).

Example of conventional designation:

Hot rolled stock, square, having side of square 46 mm, normal accuracy of rolling B as per GOST 2591 – 88, grade 18ХГТ, surface quality of group 2, heat treated T:

As well as, round having diameter 80 mm, normal accuracy of rolling B as per GOST 2590 – 88, grade 18Х2Н4МА, surface quality of group 1, mechanical properties of make 2, heat treated T:

As well as, strip having thickness 20 mm, width 75 mm as per GOST 103 – 76, grade 25ХГТ, surface quality of group 3, mechanical properties of make 1, without heat treatment:

Calibrated rolling stock, round having diameter 15 mm, with limit deviation as per h11 according to GOST 7417 – 75, grade 40ХН2МА, surface quality of group Б as per GOST 1051 – 73, with checking of mechanical properties M, cold worked H:

Rolling stock with special surface finish, round having diameter 8.5 mm with limit deviations as per h9 and surface quality of group B as per GOST 14955–77, Grade 12ХН3A with standardized hardenability П, heat treatment T:

(Amended edition, Amendment No. 5).

2. technical requirements

2.1 Structural alloy steel rolled stocks are manufactured inconformity with requirement of present standard according to production schedules, approved in established order.

(Amended edition, Amendment No. 5)

2.2 Grade and chemical composition of steel should correspond to those specified in table.1.

2.3 Mass fraction of phosphorous, sulphur, residues of copper, nickel and chromium in steel of all grades should not exceed the norms, specified in table.2.

Table 1

| Group of steel | Grade of steel | Mass fraction of elements, % |
| --- | --- | --- |
|  |  | Carbon | Silicon | Manganese | Chromium | Nickel | Molybdenum | Aluminium | Titanium | Vanadium |
| Chromium | 15Х | 0.12-0.18 | 0.17-0.37 | 0.40-0.70 | 0.70-1.00 | – | – | – | – | – |
|  | 15ХA | 0.12-0.17 | 0.17-0.37 | 0.40-0.70 | 0.70-1.00 | – | – | – | – | – |
|  | 20Х | 0.17-0.23 | 0.17-0.37 | 0.50-0.80 | 0.70-1.00 | – | – | – | – | – |
|  | 30Х | 0.24-0.32 | 0.17-0.37 | 0.50-0.80 | 0.80-1.10 | – | – | – | – | – |
|  | 30ХPA | 0.27-0.33 | 0.17-0.37 | 0.50-0.80 | 1.00-1.30 | – | – | – | – | – |
|  | 35Х | 0.31-0.39 | 0.17-0.37 | 0.50-0.80 | 0.80-1.10 | – | – | – | – | – |
|  | 38ХA | 0.35-0.42 | 0.17-0.37 | 0.50-0.80 | 0.80-1.10 | – | – | – | – | – |
|  | 40Х | 0.36-0.44 | 0.17-0.37 | 0.50-0.80 | 0.80-1.10 | – | – | – | – | – |
|  | 45Х | 0.41-0.49 | 0.17-0.37 | 0.50-0.80 | 0.80-1.10 | – | – | – | – | – |
|  | 50Х | 0.46-0.54 | 0.17-0.37 | 0.50-0.80 | 0.80-1.10 | – | – | – | – | – |
| Manganese | 15Г | 0.12-0.19 | 0.17-0.37 | 0.70-1.00 | – | – | – | – | – | – |
|  | 20Г | 0.17-0.24 | 0.17-0.37 | 0.70-1.00 | – | – | – | – | – | – |
|  | 25Г | 0.22-0.30 | 0.17-0.37 | 0.70-1.00 | – | – | – | – | – | – |
|  | 30Г | 0.27-0.35 | 0.17-0.37 | 0.70-1.00 | – | – | – | – | – | – |

Continuation table 1

| Group of steel | Grade of steel | Mass fraction of elements, % |
| --- | --- | --- |
|  |  | Carbon | Silicon | Manganese | Chromium | Nickel | Molybdenum | Aluminium | Titanium | Vanadium |
| Manganese | 35Г | 0.32-0.40 | 0.17-0.37 | 0.70-1.00 | – | – | – | – | – | – |
|  | 40Г, 40ГP | 0.37-0.45 | 0.17-0.37 | 0.70-1.00 | – | – | – | – | – | – |
|  | 45Г | 0.42-0.50 | 0.17-0.37 | 0.70-1.00 | – | – | – | – | – | – |
|  | 50Г | 0.48-0.56 | 0.17-0.37 | 0.70-1.00 | – | – | – | – | – | – |
|  | 10Г2 | 0.07-0.15 | 0.17-0.37 | 1.20-1.60 | – | – | – | – | – | – |
|  | 30Г2 | 0.26-0.35 | 0.17-0.37 | 1.40-1.80 | – | – | – | – | – | – |
|  | 35Г2 | 0.31-0.39 | 0.17-0.37 | 1.40-1.80 | – | – | – | – | – | – |
|  | 40Г2 | 0.36-0.44 | 0.17-0.37 | 1.40-1.80 | – | – | – | – | – | – |
|  | 45Г2 | 0.41-0.49 | 0.17-0.37 | 1.40-1.80 | – | – | – | – | – | – |
|  | 50Г2 | 0.46-0.55 | 0.17-0.37 | 1.40-1.80 | – | – | – | – | – | – |
|  | 47ГT | 0.44-0.52 | 0.10-0.22 | 0.90-1.20 | – | – | – | – | 0.06-0.12 | – |
| Chromium- Manganese | 18ХГ | 0.15-0.21 | 0.17-0.37 | 0.90-1.20 | 0.90-1.20 | – | – | – | – | – |
|  | 18ХГТ | 0.17-0.23 | 0.17-0.37 | 0.80-1.10 | 1.00-1.30 | – | – | – | 0.03-0.09 | – |
|  | 20ХГP | 0.18-0.24 | 0.17-0.37 | 0.70-1.00 | 0.75-1.05 | – | – | – | – | – |

Continuation table 1

| Group of steel | Grade of steel | Mass fraction of elements, % |
| --- | --- | --- |
|  |  | Carbon | Silicon | Manganese | Chromium | Nickel | Molybdenum | Aluminium | Titanium | Vanadium |
| Chromium- manganese | 27ХГP | 0.25-0.31 | 0.17-0.37 | 0.70-1.00 | 0.70-1.00 | – | – | – | – | – |
|  | 25ХГТ | 0.22-0.29 | 0.17-0.37 | 0.80-1.10 | 1.00-1.30 | – | – | – | 0.03-0.09 | – |
|  | 30ХГТ | 0.24-0.32 | 0.17-0.37 | 0.80-1.10 | 1.00-1.30 | – | – | – | 0.03-0.09 | – |
|  | 40ХГТP | 0.38-0.45 | 0.17-0.37 | 0.80-1.00 | 0.80-1.10 | – | – | – | 0.03-0.09 | – |
|  | 25ХГM | 0.23-0.29 | 0.17-0.37 | 0.90-1.20 | 0.90-1.20 | – | 0.20-0.30 | – | – | – |
|  | 38ХГM | 0.34-0.40 | 0.17-0.37 | 0.60-0.90 | 0.80-1.10 | – | 0.15-0.25 | – | – | – |
| Chrome-silicon | 33ХС | 0.29-0.37 | 1.0-14 | 0.30-0.60 | 1.30-1.60 | – | – | – | – | – |
|  | 38ХС | 0.34-0.42 | 1.0-1.4 | 0.30-0.60 | 1.30-1.60 | – | – | – | – | – |
|  | 40ХС | 0.37-0.45 | 1.2-1.6 | 0.30-0.60 | 1.30-1.60 | – | – | – | – | – |
| Chrome-molybdenum and chrome-molybdenum-vanadium | 15ХM | 0.11-0.18 | 0.17-0.37 | 0.40-0.70 | 0.80-1.10 | – | 0.40-0.55 | – | – | – |
|  | 20ХM | 0.15-0.25 | 0.17-0.37 | 0.40-0.70 | 0.80-1.10 | – | 0.15-0.25 | – | – | – |
|  | 30ХM | 0.26-0.34 | 0.17-0.37 | 0.40-0.70 | 0.80-1.10 | – | 0.15-0.25 | – | – | – |

Continuation table 1

| Group of steel | Grade of steel | Mass fraction of elements, % |
| --- | --- | --- |
|  |  | Carbon | Silicon | Manganese | Chromium | Nickel | Molybdenum | Aluminium | Titanium | Vanadium |
| Chrome-molybdenum and chrome-molybdenum-vanadium | 30ХMA | 0.26-0.33 | 0.17-0.37 | 0.40-0.70 | 0.80-1.10 | – | 0.15-0.25 | – | – | – |
|  | 35ХM | 0.32-0.40 | 0.17-0.37 | 0.40-0.70 | 0.80-1.10 | – | 0.15-0.25 | – | – | – |
|  | 38ХM | 0.35-0.42 | 0.17-0.37 | 0.35-0.65 | 0.90-1.30 | – | 0.20-0.30 | – | – | – |
|  | 30Х3MФ | 0.27-0.34 | 0.17-0.37 | 0.30-0.60 | 2.30-2.70 | – | 0.20-0.30 | – | – | 0.06-0.12 |
|  | 40ХMФA | 0.37-0.44 | 0.17-0.37 | 0.40-0.70 | 0.80-1.10 | – | 0.20-0.30 | – | – | 0.10-0.18 |
| Chrome-vanadium | 15ХФ | 0.12-0.18 | 0.17-0.37 | 0.40-0.70 | 0.80-1.10 | – | – | – | – | 0.06-0.12 |
|  | 40ХФA | 0.37-0.44 | 0.17-0.37 | 0.50-0.80 | 0.80-1.10 | – | – | – | – | 0.10-0.18 |
| Nickel-molybdenum | 15Н2M (15НM) 20Н2M (20НM) | 0.10-0.18 | 0.17-0.37 | 0.40-0.70 | – | 1.50-1.90 | 0.20-0.30 | – | – | – |
|  |  | 0.17-0.25 | 0.17-0.37 | 0.40-0.70 | – | 1.50-1.90 | 0.20-0.30 | – | – | – |
| Chrome-nickel and chrome-nickel with boron | 12ХН | 0.09-0.15 | 0.17-0.37 | 0.30-0.60 | 0.40-0.70 | 0.50-0.80 | – | – | – | – |
|  | 20ХН | 0.17-0.23 | 0.17-0.37 | 0.40-0.70 | 0.45-0.75 | 1.00-1.40 | – | – | – | – |
|  | 40ХН | 0.36-0.44 | 0.17-0.37 | 0.50-0.80 | 0.45-0.75 | 1.00-1.40 | – | – | – | – |

Continuation table 1

| Group of steel | Grade of steel | Mass fraction of elements, % |
| --- | --- | --- |
|  |  | Carbon | Silicon | Manganese | Chromium | Nickel | Molybdenum | Aluminium | Titanium | Vanadium |
| Chrome-nickel and chrome-nickel with boron | 45ХН | 0.41-0.49 | 0.17-0.37 | 0.50-0.80 | 0.45-0.75 | 1.00-1.40 | – | – | – | – |
|  | 50ХН | 0.46-0.54 | 0.17-0.37 | 0.50-0.80 | 0.45-0.75 | 1.00-1.40 | – | – | – | – |
|  | 20ХHP | 0.16-0.23 | 0.17-0.37 | 0.60-0.90 | 0.70-1.10 | 0.80-1.10 | – | – | – | – |
|  | 12ХН2 | 0.09-0.16 | 0.17-0.37 | 0.30-0.60 | 0.60-0.90 | 1.50-1.90 | – | – | – | – |
|  | 12ХН3A | 0.09-0.16 | 0.17-0.37 | 0.30-0.60 | 0.60-0.90 | 2.75-3.15 | – | – | – | – |
|  | 20ХН3A | 0.17-0.24 | 0.17-0.37 | 0.30-0.60 | 0.60-0.90 | 2.75-3.15 | – | – | – | – |
|  | 30ХН3A | 0.27-0.33 | 0.17-0.37 | 0.30-0.60 | 0.60-0.90 | 2.75-3.15 | – | – | – | – |
|  | 12Х2Н4A | 0.09-0.15 | 0.17-0.37 | 0.30-0.60 | 1.25-1.65 | 3.25-3.65 | – | – | – | – |
|  | 20Х2Н4A | 0.16-0.22 | 0.17-0.37 | 0.30-0.60 | 1.25-1.65 | 3.25-3.65 | – | – | – | – |
| Chrome-silicon-manganese and chrome-silicon-manganese-nickel | 20ХГСA | 0.17-0.23 | 0.9-1.2 | 0.80-1.10 | 0.80-1.10 | – | – | – | – | – |
|  | 25ХГСA | 0.22-0.28 | 0.9-1.2 | 0.80-1.10 | 0.80-1.10 | – | – | – | – | – |
|  | 30ХГС | 0.28-0.35 | 0.9-1.2 | 0.80-1.10 | 0.80-1.10 | – | – | – | – | – |
|  | 30ХГСA | 0.28-0.34 | 0.9-1.2 | 0.80-1.10 | 0.80-1.10 | – | – | – | – | – |

Continuation table 1

| Group of steel | Grade of steel | Mass fraction of elements, % |
| --- | --- | --- |
|  |  | Carbon | Silicon | Manganese | Chromium | Nickel | Molybdenum | Aluminium | Titanium | Vanadium |
| Chrome-silicon-manganese and chrome-silicon-manganese-nickel | 35ХГСA | 0.32-0.39 | 1.1-1.4 | 0.80-1.10 | 1.10-1.40 | – | – | – | – | – |
|  | 30ХГСН2A (30ХГСНA) | 0.27-0.34 | 0.9-1.2 | 1.00-1.30 | 0.90-1.20 | 1.4-1.8 | – | – | – | – |
| Chrome-manganese nickel and chrome-manganese-nickel with titanium and boron | 15ХГН2TA (15ХГНTA) | 0.13-0.18 | 0.17-0.37 | 0.70-1.00 | 0.70-1.00 | 1.4-1.8 | – | – | 0.03-0.09 | – |
|  | 20ХГНP | 0.16-0.23 | 0.17-0.37 | 0.70-1.00 | 0.70-1.10 | 0.80-1.10 | – | – | – | – |
|  | 20ХГНTP | 0.18-0.24 | 0.17-0.37 | 0.80-1.10 | 0.40-0.70 | 0.40-0.70 | – | – | 0.03-0.09 | – |
|  | 38ХГН | 0.35-0.43 | 0.17-0.37 | 0.80-1.10 | 0.50-0.80 | 0.70-1.00 | – | – | – | – |
|  | 14ХГН | 0.13-0.18 | 0.17-0.37 | 0.70-1.00 | 0.80-1.10 | 0.80-1.10 | – | – | – | – |
|  | 19ХГН | 0.16-0.21 | 0.17-0.37 | 0.70-1.10 | 0.80-1.10 | 0.80-1.10 | – | – | – | – |
| Chrome- nickel- molybdenum | 20ХН2M (20ХНM) | 0.15-0.22 | 0.17-0.37 | 0.40-0.70 | 0.40-0.60 | 1.6-2.0 | 0.20-0.30 | – | – | – |
|  | 30ХН2МА (30ХНMA) | 0.27-0.34 | 0.17-0.37 | 0.30-0.60 | 0.60-0.90 | 1.25-1.65 | 0.20-0.30 | – | – | – |
|  | 38Х2Н2MA (38ХНMA) | 0.33-0.40 | 0.17-0.37 | 0.25-0.50 | 1.30-1.70 | 1.3-1.7 | 0.20-0.30 | – | – | – |

Continuation table 1

| Group of steel | Grade of steel | Mass fraction of elements, % |
| --- | --- | --- |
|  |  | Carbon | Silicon | Manganese | Chromium | Nickel | Molybdenum | Aluminium | Titanium | Vanadium |
| Chrome- nickel molybdenum | 40ХН2МА (40ХНMA) | 0.37-0.44 | 0.17-0.37 | 0.50-0.80 | 0.60-0.90 | 1.25-1.65 | 0.15-0.25 | – | – | – |
|  | 40Х2Н2MA (40Х1НВA) | 0.35-0.42 | 0.17-0.37 | 0.30-0.60 | 1.25-1.65 | 1.35-1.75 | 0.20-0.30 | – | – | – |
|  | 38ХН3MA | 0.33-0.40 | 0.17-0.37 | 0.25-0.50 | 0.80-1.20 | 2.75-3.25 | 0.20-0.30 | – | – | – |
|  | 18Х2Н4МА (18Х2Н4ВA) | 0.14-0.20 | 0.17-0.37 | 0.25-0.55 | 1.35-1.65 | 4.0-4.4 | 0.30-0.40 | – | – | – |
|  | 25Х2Н4МА (25Х2Н4ВA) | 0.21-0.28 | 0.17-0.37 | 0.25-0.55 | 1.35-1.65 | 4.0-4.4 | 0.30-0.40 | – | – | – |
| Chrome-nickel-molybdenum-vanadium and chrome-nickel-vanadium | 30ХН2MФA (30ХН2ВФА) | 0.27-0.34 | 0.17-0.37 | 0.30-0.60 | 0.60-0.90 | 2.0-2.4 | 0.20-0.30 | – | – | 0.10-0.18 |
|  | 36Х2Н2MФA (36ХН1MФA) | 0.33-0.40 | 0.17-0.37 | 0.25-0.50 | 1.30-1.70 | 1.30-1.70 | 0.30-0.40 | – | – | 0.10-0.18 |
|  | 38ХН3МФA | 0.33-0.40 | 0.17-0.37 | 0.25-0.50 | 1.20-1.50 | 3.0-3.5 | 0.35-0.45 | – | – | 0.10-0.18 |
|  | 45ХН2MФA (45ХMФA) 20ХН4ФA | 0.42-0.50 | 0.17-0.37 | 0.50-0.80 | 0.80-1.10 | 1.3-1.8 | 0.20-0.30 | – | – | 0.10-0.18 |
|  |  | 0.17-0.24 | 0.17-0.37 | 0.25-0.55 | 0.70-1.10 | 3.75-4.15 | – | – | – | 0.10-0.18 |
| Chrome-aluminum and chrome-aluminum- molybdenum | 38Х2МЮА (38ХМЮА) | 0.35-0.42 | 0.20-0.45 | 0.30-0.60 | 1.35-1.65 | – | 0.15-0.25 | 0.7-1.1 | – | – |

Continuation table 1

| Group of steel | Grade of steel | Mass fraction of elements, % |
| --- | --- | --- |
|  |  | Carbon | Silicon | Manganese | Chromium | Nickel | Molybdenum | Aluminium | Titanium | Vanadium |
| chrome-manganese-nickel with molybdenum and titanium | 20ХГНM | 0.18-0.23 | 0.17-0.37 | 0.70-1.10 | 0.40-0.70 | 0.40-0.70 | 0.15-0.25 | – | – | – |
|  | 40ХГНM | 0.37-0.43 | 0.17-0.37 | 0.50-0.80 | 0.60-0.90 | 0.70-1.10 | 0.15-0.25 | – | – | – |
|  | 25ХГНMT | 0.23-0.29 | 0.17-0.37 | 0.50-0.80 | 0.40-0.60 | 0.80-1.10 | 0.40-0.50 | – | 0.04-0.09 | – |

Note:-

- Chemical composition of steel – category Ш should correspond the norms specified in table 1 for the corresponding grade of steel.

- In the denotation of grade, the first two digits specify the average contents of carbon in hundreds fraction of percent, letters, after digit denote: P – Boron, Ю – aluminium, С- silicon, T – Titanium, Ф– Vanadium, Х – Chromium, Г – manganese, Н – Nickel, M – Molybdenum, В – Tungsten. The digit after letter specifies the approximate contents of alloying elements in complete units. The absence of digits denotes that this alloying element upto 1.5% is contained in the grade. The letter “A” at the end of description of grade denotes the «high quality steel». Very high quality steel is denoted by the letter Ш, after dash at the end of description of grade for example – quality – 30ХГС, high quality – 30ХГСA; Very high quality – 30ХГС – Ш, 30ХГСA – Ш.

The denotations of grades of steel corresponding to already existing GOST 4343 – 61 and technical specification are given in the brackets.

- The steel of grades 30Г2, 35Г2, 40Г2, 45Г2, 50Г2 as per the requirements of customer may be supplied with contents of manganese 1.2 – 1.6%

- For steel of grade 20ХГP, 20ХНP, 20ХГНР, 27ХГP and 18Х2Н4МА, Technical addition of titanium as per calculation (without calculation of loss) upto 0.06 % is permitted.

- In steel, containing letter P in the denotation of grade, boron is added as per the calculation (without calculating the loss) in quantity not more  than 0.005% In this case, its residual contents in steel should not be less than 0.0010%

- In steel, alloy with molybdenum, grade 38ХM, 30ХН2МА, 30Х2Н2MA, 40Х2Н2MA, 38ХН3MA, 18Х2Н4МА, 25Х2Н4МА,  30ХН2MФA partial or complete substitution of molybdenum by tungsten is permitted.

During partial substitution of molybdenum by tungsten, one part by weight of molybdenum is substituted by three parts by weight of tungsten; In this case, the total contents of molybdenum and tungsten should correspond to the norms specified in table 1.

According to the requirement of customer, the steels with grade 38ХВ, 30ХН2ВA, 30Х2Н2ВA, 40Х2Н2ВA, 38ХH3BA, 18Х2Н4ВA, 25Х2Н4ВA, and 30ХН2ВФА is manufactured.

Mass fraction of tungsten in these steels should be as follows:

30ХВ		0.50 – 0.80%					38ХН3ВA	 0.50 – 0.80%

30ХН2ВA	0.50 – 0.80%					18Х2Н4ВA	 0.80 – 1.2 %

38Х2Н2ВA	0.50 – 0.80%					25Х2Н4BA	 0.80 – 1.2%

40Х2Н2ВA	0.60 – 0.90%					30ХН2ВФА	 0.50 – 0.80%

In specified grade of steel, partial replacement of tungsten by residual molybdenum is permitted at the rate of: one part by weight of molybdenum is substituted by three parts by weight of tungsten. In this case, mass fraction of tungsten should not be less than:

38ХВ		0.30%							38ХН3ВA	  0.30%

30ХН2В2A	0.30%							18Х2Н4ВA	  0.50%

38Х2Н2ВA	0.30%							25Х2Н4ВA	  0.50%

40Х2Н2ВA	0.40%							30ХН2ВФА	  0.30%

7. Presence of tungsten upto 0.20%, molybdenum upto 0.15%, titanium upto 0.03% (excluding the steels of grade, mentioned in note No 4) and vanadium upto 0.05 % in steels not alloyed by these elements is not the reason for rejection.

8. Steel grade 38ХН3МФA as per order of customer may be manufactured with mass fraction of molybdenum 0.20-0.30%.

9. Mass fraction of nitrogen in oxygen in converter steel should not exceed for thin sheet of rolling and strip – 0.006 %; for other type of rolling – 0.008%.

10. In accordance with the order, in steel grade 15Х, 20Х, 30Х, 35Х, 40Х, 45Х, 40ХН, 15ХФ, 30ХMA mass fraction of silicon 0.10 – 0.37% and in steel grade 20Х and 30Х mass fraction of manganese 0.40-0.80%.

11. As per the requirements of customer, in steel non – alloyed by chromium and nickel, mass fraction of manganese may be decreased to value of manganese equivalent, which is equal to:

ЭМ = 0.3 (Cч, %) + 0.5 (Ni, %) + 0.7 (Cи, %),

Where Cч, Ni, Cи – residual mass fraction of chromium, nickel and copper should not exceed the norms of table 2. In this case, mass fraction of manganese in steel should not be less than 0.35 %.

(Amended edition, Amendment No. 1, 2, 4, 5)

Table 2

| Category of steel | Mass fraction of elements in % not more than. |
| --- | --- |
|  | Phosphorous | Sulphur | Copper | Nickel | Chromium |
| Quality | 0.035 | 0.035 | 0.30 | 0.30 | 0.30 |
| High quality | 0.025 | 0.025 | 0.30 | 0.30 | 0.30 |
| Very high quality | 0.025 | 0.015 | 0.25 | 0.30 | 0.30 |

Note: -

1. For high quality steels, melted in the main martin furnaces and in the furnaces with acid lining content of phosphorus up to 0.030% is permitted.

In accordance with order in steel, manufactured with scrap process and scrap - ore process, residual mass fraction of nickel and chromium should not more than 0.40 % each.

2.  Quality steel of all grades can be manufactured with mass fraction of sulphur and phosphorus in accordance with requirements of tables 2 for high quality steel.  In this case, letter A is added to nomenclature of grade of steel.

(Amended edition, Amendment No.  2.5)

2.4 In finished roll and forgings, while observing the norm of mechanical properties and other requirements of present standard, deviations on chemical composition are allowed. Permissible deviation should correspond to those specified in table 3.

Table 3

| Name of element | Upper limit of mass fraction of elements, in % | Permissible deviation, in % | Name of element | Upper limit of mass fraction of elements, in % | Permissible deviation, in % |
| --- | --- | --- | --- | --- | --- |
| Carbon | As per table 1 | ( 0.01 | Vanadium | 0.06 – 0.12 0.10 – 0.18 | + 0.02 ( 0.02 |
| Aluminium | As per table 1 | ( 0.10 | Manganese | Less than 1.0 1.0 and above | ( 0.02 ( 0.05 |
| Silicon | Less than 1.0 1.0 and above | ( 0.02 ( 0.05 | Nickel | Less than 2.5 2.5 and above | - 0.05 - 0.10 |
| Titanium | As per table 1 | ( 0.02 | Molybdenum | As per table 1 | ( 0.02 |
| Chromium | Less than 1.0 1.0 and above | ( 0.02 ( 0.05 | Tungsten | As per table 1 | ( 0.05 |

Note:-  In quality steels, the deviation on contents of Sulphur and phosphorus by not more than + 0.005% of each is allowed as per the approval of customer.

(Amended addition, Amendment No.  2)

  - In accordance with the indent, the hot rolled and forged roll stock are supplied both in heat treated condition (annealed, highly tempered or normalized with high tempering) and without heat treatment; calibrated and with special surface finish,

roll stock is manufactured by cold worked or heat treated condition (annealed, tempered, normalized, hardened and tempered).

  - The brinell hardness (HB) of annealed or high tempered roll stock with diameter or thickness above 5 mm should correspond to the norms specified in table 4.

Table 4

| Group of steel | Grade of steel | Diameter of indent, mm, not less than | Hardness number, HB, maximum |
| --- | --- | --- | --- |
| Chromium | 15Х | 4.5 | 179 |
|  | 15ХA | 4.5 | 179 |
|  | 20Х | 4.5 | 179 |
|  | 30Х | 4.4 | 187 |
|  | 30ХPA | 3.9 | 241 |
|  | 35Х | 4.3 | 197 |
|  | 38ХA | 4.2 | 207 |
|  | 40Х | 4.1 | 217 |
|  | 45Х | 4.0 | 229 |
|  | 50Х | 4.0 | 229 |
| Manganese | 15Г | 4.7 | 163 |
|  | 20Г | 4.5 | 179 |
|  | 25Г | 4.3 | 197 |
|  | 30Г | 4.3 | 197 |
|  | 35Г | 4.2 | 207 |
|  | 40Г, 40 ГP | 4.2 | 207 |
|  | 45Г | 4.0 | 229 |
|  | 50Г | 4.0 | 229 |
|  | 10Г2 | 4.3 | 197 |
|  | 30Г2 | 4.2 | 207 |
|  | 35Г2 | 4.2 | 207 |
|  | 40Г2 | 4.1 | 217 |
|  | 45Г2 | 4.0 | 229 |
|  | 50Г2 | 4.0 | 229 |
|  | 47ГT | 3.8 | 255 |
| Chrome-manganese | 18ХГ | 4.4 | 187 |
|  | 18ХГТ | 4.1 | 217 |
|  | 20ХГP | 4.3 | 197 |
|  | 27ХГP | 4.1 | 217 |
|  | 25ХГТ | 4.1 | 217 |
|  | 30ХГТ | 4.0 | 229 |
|  | 40ХГТP | 4.0 | 229 |
|  | 38ХГM | + | + |

Continuation of table 4.

| Group of steel | Grade of steel | Diameter of indent, mm, not more than | Hardness number, HB, not more than |
| --- | --- | --- | --- |
| Chrome – silicon | 33ХС | 3.9 | 241 |
|  | 38ХС | 3.8 | 255 |
|  | 40ХС | 3.8 | 255 |
| Chrome - molybdenum and chrome - molybdenum - vanadium | 15ХМ | 4.5 | 179 |
|  | 20ХМ | 4.5 | 179 |
|  | 30ХМ | 4.0 | 229 |
|  | 30ХМА | 4.0 | 229 |
|  | 35ХМ | 3.9 | 241 |
|  | 38ХМ | 3.9 | 241 |
|  | 30Х3МФ | 4.0 | 229 |
|  | 40ХМФА | 3.7 | 269 |
| Chrome - vanadium | 15ХФ | 4.4 | 187 |
|  | 40ХФА | 3.9 | 241 |
| Nickel - molybdenum | 15Н2М (15НМ) | 4.3 | 197 |
| Chrome – nickel and chrome – nickel with boron | 12ХН | + | + |
|  | 20ХН | 4.3 | 197 |
|  | 40ХН | 4.2 | 207 |
|  | 45ХН | 4.2 | 207 |
|  | 50ХН | 4.2 | 207 |
|  | 12ХН2 | 4.2 | 207 |
|  | 12ХН3А | 4.1 | 217 |
|  | 20ХН3А | 3.8 | 255 |
|  | 12Х2Н4А | 3.7 | 269 |
|  | 20Х2Н4А | 3.7 | 269 |
|  | 30ХН3А | 3.9 | 241 |
| Chrome-silicon-manganese and chrome-silicon-manganese-nickel | 20ХГСА | 4.2 | 207 |
|  | 25ХГСА | 4.1 | 217 |
|  | 30ХГС | 4.0 | 229 |
|  | 30ХГСА | 4.0 | 229 |
|  | 30ХГСН2А (30ХГСНА) | 3.8 | 255 |
|  | 35ХГСА | 3.9 | 241 |
| Chrome-manganese-nickel and chrome-manganese-nickel with titanium and boron | 15ХГН2ТА (15ХГНТА) | 3.7 | 269 |
|  | 20ХГНP | 4.3 | 197 |
|  | 14ХГН | + | + |
|  | 19ХГН | + | + |
|  | 38ХГН | 4.0 | 229 |

Continuation of table 4.

| Group of steel | Grade of steel | Diameter of indentation, mm, not less than | Hardness number, HB, not more than |
| --- | --- | --- | --- |
| Chrome – nickel - molybdenum | 20ХН2М (20ХНМ) | 4.0 | 229 |
|  | 30ХН2МА (30ХНМА) | 3.9 | 241 |
|  | 38Х2Н2МА (38ХНМА) | 3.7 | 269 |
|  | 40ХН2МА (40ХНМА) | 3.7 | 269 |
|  | 40Х2Н2МА (40Х1НВА) | 3.8 | 255 |
|  | 38ХН3МА | 3.7 | 269 |
|  | 18Х2Н4МА (18Х2Н4ВА) | 3.7 | 269 |
|  | 25Х2Н4МА (25Х2Н4ВА) | 3.7 | 269 |
| Chrome – nickel – molybdenum – silicon and chrome – nickel - silicon | 30ХН2МФА | 3.7 | 269 |
|  | 36Х2Н2МФА (36ХН1МФА) | 3.7 | 269 |
|  | 38ХН3МФА | 3.7 | 269 |
|  | 45ХН2МФА (45ХНМФА) | 3.7 | 269 |
|  | 20ХН4ФА | 3.7 | 269 |
| Chrome – aluminium and chrome aluminium with molybdenum | 38Х2МЮА (38ХМЮА) | 4.0 | 229 |
| Chrome – manganese – nickel with molybdenum and titanium | 20ХГНМ | + | + |
|  | 40ХГНМ | + | + |
|  | 25ХГНМТ | + | + |

Note:

- Upon agreement between manufacturer and customer, it is permitted to manufacturer the roll stock without annealing and high tempering with hardness, corresponding to norms, indicated in table 4.

- The hardness of calibrated roll in annealed or high tempered condition as well as hot rolled steel, normalized with subsequent high tempering can exceed the hardness value by 15 units of HB specified in table 4.

- The hardness of roll stock of grade 20ХНP, 25ХГM, 20Н2M (20НM) and 20ХГНTP is set as per agreement between manufacturer and customer.

- Hardness norm for roll stock, manufactured in normalized condition are set as per the agreement with manufacturer and customer.

- (Delete, Amendment No. 3).

6. Sign “+” denotes that up to 01. 01. 92 hardness are determined for the accumulation of data  and results of tests, indicated in the document about the quality.

2.5, 2.6 (Amended edition, Amendment No.  1, 2, 3, 4, 5).

2.7. The hardness of work hardened steel with diameter or thickness above 5 mm, should be not more than BHN 269 (Diameter of indentation, not less than 3.7 mm) or set as per the agreement between manufacturer and customer, except the roll of grades 15Х, 15ХA, 20Х, 30Х, 35Х, 15Г, 18ХГТ, 15ХФ, 38Х2МЮА (38ХМЮА), the hardness of which should correspond to the norms specified in table5.

Table 5.

| Grades of steel | Diameter of indentation, in mm, not less than | Hardness number in HB, not more than |
| --- | --- | --- |
| 15Х, 15ХA | 4.1 | 217 |
| 20Х | 4.0 | 229 |
| 30Х | 3.9 | 241 |
| 35Х | 3.8 | 255 |
| 15Г | 4.2 | 207 |
| 18ХГТ | 4.0 | 229 |
| 15ХФ | 4.1 | 217 |
| 30Х2МЮА (38ХМЮА) | 3.8 | 255 |

(Amended edition, Amendment No.  2, 5)

2.8.The hardness of annealed and cold worked calibrated steel and with special surface finish of roll with diameter upto 5 mm inclusive as well as hardening with tempering the roll of all dimensions is set as per the agreement between manufacturer and customer.

(Amended edition, Amendment No.  5)

2.9.The mechanical properties of roll at normal temperature, to be determined for longitudinal heat-treated samples or samples, manufactured from heat-treated blanks should correspond to the norms specified in table 6. Inspection of mechanical properties of calibrated steel and with special surface finish of roll is carried out according to the requirement of customer with the specification in conventional designation of letter M.

Roll stock made up of chromium nickel molybdenum, chromium nickel molybdenum steels are tested additionally for impact strength at normal temperature for samples of type 11 as per GOST 9454 – 78

Note: - Samples for mechanical tests of roll, to be manufactured in the hardened and tempered conditions, are not subjected to heat treatment; the norms of mechanical properties are set as per the agreement between manufacturer and customer.

Table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalizing | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |  |
| Chromium | 15Х 15ХА | 880 | 770- 820 | Water or oil | 180 | Air or oil | 490 (50) | 690 (70) | 12 | 45 | 69 (7) | 15 |
|  | 20Х | 880 | 770- 820 | Water or oil | 180 | Air or oil | 635 (65) | 780 (80) | 11 | 40 | 59 (6) | 15 |
|  | 30Х | 860 | — | Oil | 500 | Water or oil | 685 (70) | 880 (90) | 12 | 45 | 69 (7) | 25 |
|  | 30ХPА | 900 Air | 860 | Oil | 200 | Air | 1275 (130) | 1570 (160) | 9 | 40 | 49 (5) | - |
|  | 35Х | 860 | — | Oil | 500 | Water or oil | 735 (75) | 910 (93) | 11 | 45 | 69 (7) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |  |
| Chromium | 38ХA | 860 | - | Oil | 550 | Water or oil | 785 (80) | 930 (95) | 12 | 50 | 88 (9) | 25 |
|  | 40Х | 860 | - | Oil | 500 | Water or oil | 785 (80) | 980 (100) | 10 | 45 | 59 (6) | 25 |
|  | 45Х | 840 | - | Oil | 520 | Water or oil | 835 (85) | 1030 (105) | 9 | 45 | 49 (5) | 25 |
|  | 50Х | 830 | - | Oil | 520 | Water or oil | 885 (90) | 1080 (110) | 9 | 40 | 39 (4) | 25 |
| Mang-anese | 15Г | 880 | - | Air | - | - | 245 (25) | 410 (42) | 26 | 55 | - | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Manganese | 20Г | 880 | - | Air | - | - | 275 (28) | 450 (46) | 24 | 50 | - | 25 |
|  | 25Г | 880 | - | Water or air | 560 | Air | 295 (30) | 490 (50) | 22 | 50 | 88 (9) | 25 |
|  | 30Г | 860 | - | Water or air | 600 | Air | 315 (32) | 540 (55) | 20 | 45 | 78 (8) | 25 |
|  | 35Г | 860 | - | Water or air | 600 | Air | 335 (34) | 560 (57) | 18 | 45 | 69 (7) | 25 |
|  | 40Г, 40ГP | 860 | - | Water or air | 600 | Air | 355 (36) | 590 (60) | 17 | 45 | 59 (6) | 25 |
|  | 45Г | 850 | - | Oil or air | 600 | Air | 375 (38) | 620 (63) | 15 | 40 | 49 (5) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Manganese | 50Г | 850 | - | Oil or air | 600 | Air | 390 (40) | 650 (66) | 13 | 40 | 39 (4) | 25 |
|  | 47ГT | 820-870 | - | Air | - | - | 375 (38) 2) 390 (40) | 620 (63) 640 (65) | 15 12 | 40 30 | - - | 25 25 |
|  | 10Г2 | 920 | - | Air | - | - | 245 (25) | 420 (43) | 22 | 50 | - | 25 |
|  | 30Г2 | 880 | - | Oil or air | 600 | Air | 345 (35) | 590 (60) | 15 | 45 | - | 25 |
|  | 35Г2 | 870 | - | Oil or air | 650 | Air | 365 (37) | 620 (63) | 13 | 40 | - | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Manganese | 40Г2 | 860 | _ | Oil or air | 650 | Air | 380 (39) | 660 (67) | 12 | 40 | _ | 25 |
|  | 45Г2 | 850 | — | Oil or air | 650 | Air | 400 (41) | 690 (70) | 11 | 40 | — | 25 |
|  | 50Г2 | 840 | — | Oil or air | 650 | Air | 420 (43) | 740 (75) | 11 | 35 | — | 25 |
| Chrome- manganese | 18ХГ | 880 | _ | Oil | 200 | Air or oil | 735 (75) | 880 (90) | 10 | 40 | _ | 15 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Chrome - Manganese | 18ХГТ | 880 - 950 Air | 870 | Oil | 200 | Air or water | 885 (90) | 980 (100) | 9 | 50 | 78 (8) | - |
|  | 20ХГP | 880 | - | Oil | 200 | Air or oil | 785 (80) | 980 (100) | 9 | 50 | 78 (8) | 15 |
|  | 27ХГP | 870 | - | Oil | 200 | Air | 1175 (120) | 1370 (140) | 8 | 45 | 59 (6) | - |
|  | 25ХГТ | 880-950 Air | 850 | Oil | 200 | Water, oil or air | 980 (100) 2) 1080 (110) | 1270 (130) 1470 (150) | 10 9 | 50 45 | 69 (7) 59 (6) | - - |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Chrome - Manganese | 30ХГТ | 880 - 950 Air | 850 | Oil | 200 | Water, oil or air | 1275 (130) | 1470 (150) | 9 | 40 | 59 (6) | - |
|  | 40ХГТР | 840 | - | Oil | 550 | Water, oil or air | 785 (80) | 980 (100) | 11 | 45 | 78 (8) | 25 |
|  | 25ХГМ | 860 | - | Oil | 200 | Air | 1080 (110) | 1180 (120) | 10 | 45 | 78 (8) | - |
|  | 38ХГМ | 870 | - | Oil | 580-620 | Air | 785 (80) | 930 (95) | 11 | - | 78 (8) | 25 |

# Text boxes

GOST 4543-71