Hexagon Bolts with reduced head,

Product Grade A

Construction and Dimensions

GOST 7808 - 70

# Translated by:

M/s SWYAZ

2/453, Viram Khand, Gomti Nagar

# Lucknow – 226010

(: 0522–3098139 / 2345145	                                                                                       Visit us:

http\\:www.swyaz.com

# Inter State Standards

Hexagon bolts with reduced head,

product grade A

## GOST

Construction and Dimensions           			    	    7808 - 70

ОКП 12 8200

Date of introduction 01.01.72

1.	This standard pertains to bolts with hexahedral-reduced head of precision class A with thread diameter from 8 to 48 mm.

(Amended edition, Amendment No.4).

2.	Design and sizes of bolts should correspond to those indicated on the drawing and in table 1, 2.

(Amended edition, Amendment No.2 - 6).

3.	Threads - as per GOST 24705. Run-outs and under-cuts of threads - as per GOST 27148. Ends of bolts - as per GOST 12414.

(Amended edition, Amendment No.5).

3a.	Radius for head – as per GOST 24670.

3b.	Tolerance of dimensions, deviation of forms and location of surfaces not established according to this standard, as per GOST 1759.1.

3c.	Permissible defects at surfaces of bolts and methods of inspection – as per GOST 1759.2.

3a – 3b.   (Introduced additionally, Amendment No.4).

4.	By agreement between manufacturer and customer it is permitted to manufacture:

- bolts of make 1 and 2 with head thickness, equal to k1;

- bolts with nominal thread diameter from 36 to 48 mm with  2 mm pitch of thread.

(Amended edition, Amendment No.2, 4).

5.	Version of make of head is set by manufacturer.

5a.	According to agreement between manufacturer and user, manufacturing bolts with diameter of smooth part of rod d1, approximately equal to mean thread diameter, is permitted.

5b.	For application of signs of marking, it is permitted to manufacturer bolts of make 1 and 2 with hole on face with sizes, with not decreasing strength of head, during this depth of hole should not be more than 0.4 k.

5a, 5b. (Introduced additionally, Amendment No.5).

6.	Technical requirements – as per GOST 1759.0.

7.	(Deleted, Amendment No.2).

8.	Mass of bolts specified in appendix 1.

9.	(Deleted, Amendment No.4).

GOST 7808-70 Page 2

### GOST 7808-70 Page 3

GOST 7808-70 Page 4

GOST 7808-70 Page 5

GOST 7808-70 Page 6

## Mass of steel bolt (make 1) with thick pitch of thread

Appendix 1

Reference

For determination of mass of bolts from other materials of mass value, specified in table, should be

Multiplied with coefficient : 0.356 – for aluminum alloy; 1.080 – for brasses.

Appendix 1. (Amended edition, Amendment No. 5, 6).

Appendix 2. (Deleted, Amendment No.6).

GOST 7808-70 Page 7

## Supersedes GOST 7808-62

Reference normative-technical documents

| Description of HTД, where reference are given | Number of Point | Description of HTД, where reference are given | Number of Point |
| --- | --- | --- | --- |
| GOST 1759.0-87 GOST 1759.1-82 GOST 1759.2-82 GOST 12414-94 | 6 3б 3в 3 | GOST 24670-81 GOST 24705-81 GOST 27148-86 | 3а 3 3 |

Reprinted with Amendment No. 2, 3, 4, 5, 6, approved in February 1974, March 1981, May 1985, March 1989, June 1995  (ИУС 3 – 74, 6 – 81, 8 – 85, 6 – 89, 9 - 95)

# Text boxes

Length of thread and distance from supporting surface of head upto axis of hole l1 at nominal diameter of thread d(signs and marks of bolts with thread an entire length of shaft)

Length of thread and distance from supporting surface of head upto axis of hole l1 at nominal diameter of thread d(signs and marks of bolts with thread an entire length of shaft)

Bolts M12-6gx60.58 GOST 7808-70

Theoretical mass of 1000 piece of bolts, kg=, at nominal diameter of thread d, mm