Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross sectional dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalizing | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |  |
| Chromium-silicon | 33XC | 920 | - | Water or oil | 630 | Water or oil | 685 (70) | 880 (90) | 13 | 50 | 78 (8) | 25 |
|  | 38XC | 900 | - | Water or oil | 630 | Water or oil | 735 (75) | 930 (95) | 12 | 50 | 69 (7) | 25 |
|  | 40XC | 900 | - | Water or oil | 540 | Water or oil | 1) 1080 (110) | 1230 (125) | 12 | 40 | 34 (3.5) | 25 |
|  |  | Austempering at 900-910(C in nitrate at 330-350(C and then cooling in air | 2) 1080 (110) | 1230 (125) | 12 | 40 | 49 (5) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |  |
| Chrome-molybdenum and chrome-molybdenum-vanadium | 15XM | 880 | - | Air | 650 | Air | 275 (28) | 440 (45) | 21 | 55 | 118 (12) | 30 |
|  | 20XM | 880 | - | Water or oil | 500 | Air | 590 (60) | 780 (80) | 12 | 50 | 88 (9) | 15 |
|  | 30ХM | 880 | - | Oil | 540 | Water or oil | 735 (75) | 930 (95) | 11 | 45 | 78 (8) | 15 |
|  | 30XMA | 880 | - | Oil | 540 | Water or oil | 735 (75) | 930 (95) | 12 | 50 | 88 (9) | 15 |
|  | 35XM | 850 | - | Oil | 560 | Water or oil | 835 (85) | 930 (95) | 12 | 45 | 78 (8) | 25 |
|  | 38XM | 850 | - | Oil | 580 | Air | 885 (90) | 980 (100) | 11 | 45 | 69 (7) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Chrome-molybdenum and chrome-molybdenum-vanadium | 30X3MФ | 870 | - | Oil | 620 | Water or oil | 835 (85) | 980 (100) | 12 | 55 | 98 (10) | 25 |
|  | 40XMФA | 860 | - | Oil | 580 | Oil | 930 (95) | 1030 (105) | 13 | 50 | 88 (9) | 25 |
| Chrome - vanadium | 15XФ | 880 | 760-810 | Water or oil | 180 | Air or oil | 540 (55) | 740 (75) | 13 | 50 | 78 (8) | 15 |
|  | 40XФA | 880 | - | Oil | 650 | Water or oil | 735 (75) | 880 (90) | 10 | 50 | 88 (9) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Nickel- molybdenum | 15H2M (15HM) | 860 | 770-820 | Oil | 180 | Air | 635 (65) | 830 (85) | 11 | 50 | 78 (8) | 15 |
|  | 20H2M (20HM) | 860 | - | Oil | 180 | Air | 685 (70) | 880 (90) | 10 | 50 | 78 (8) | 15 |
| Chrome-nickel and chrome-nickel with boron | 12XH | 910 | - | Water or oil | 150-180 | Air | 440 (45) | 640 (65) | 10 | - | 88 (9) |  |
|  | 20XH | 860 | 760-810 | Water or oil | 180 | Water, oil or air | 590 (60) | 780 (80) | 14 | 50 | 78 (8) | 15 |
|  | 40XH | 820 | - | Water or oil | 500 | Water or oil | 785 (80) | 980 (100) | 11 | 45 | 69 (7) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Chrome-nickel and chrome-nickel with boron | 45XH | 820 | _ | Water or oil | 530 | Water or oil | 835 (85) | 1030 (105) | 10 | 45 | 69 (7) | 25 |
|  | 50XH | 820 | — | Water or oil | 530 | Water or oil | 885 (90) | 1080 (110) | 9 | 40 | 49 (5) | 25 |
|  | 20XHP | 930-950 air | 780-830 | Oil | 200 | Air or oil | 980 (100) | 1180 (120) | 10 | 50 | 88 (9) | 15 |
|  | 12XH2 | 860 | 760-810 | Water or oil | 180 | Air or oil | 590 (60) | 780 (80) | 12 | 50 | 88 (9) | 15 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross sectional dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalizing | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |  |
| Chrome-nickel and chrome-nickel with boron | 12XH3A | 860 | 760- 810 | Water or oil | 180 | Air or oil | 685 (70) | 930 (95) | 11 | 55 | 88 (9) | 15 |
|  | 20XH3A | 820 | - | Oil | 500 | Water or oil | 735 (75) | 930 (95) | 12 | 55 | 108 (11) | 15 |
|  | 12X2H4A | 860 | 760-800 | Oil | 180 | Air or oil | 930 (95) | 1130 (115) | 10 | 50 | 88 (9) | 15 |
|  | 20X2H4A | 860 | 780 | Oil | 180 | Air or oil | 1080 (110) | 1270 (130) | 9 | 45 | 78 (8) | 15 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross sectional dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |  |
|  | 30XH3A | 820 | - | Oil | 530 | Water or oil | 785 (80) | 980 (100) | 10 | 50 | 78 (8) | 25 |
| Chrome-silicon-manganese and chrome-silicon-manganese-nickel | 20XГCA | 880 | - | Oil | 500 | Water or oil | 635 (65) | 780 (80) | 12 | 45 | 69 (7) | 15 |
|  | 25XГCA | 880 | - | Oil | 480 | Water or oil | 835 (85) | 1080 (110) | 10 | 40 | 59 (6) | 15 |
|  | 30XГC | 880 | - | Oil | 540 | Water or oil | 835 (85) | 1080 (110) | 10 | 45 | 44 (4.5) | 25 |
|  | 30XГCA | 880 | - | Oil | 540 | Water or oil | 835 (85) | 1080 (110) | 10 | 45 | 49 (5) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Chrome-silicon-manganese and chrome-silicon-manganese-nickel | 35XГCA | Austempering at temperature 880(C in the mixture of potassium and sodium nitrate, having temperature 280-310(C, cooling in air |  |  |  |  |  |  |
|  |  | 950 oil 700 air | 890 | Oil | 230 | Air or oil | 1275 (130) | 1620 (165) | 9 | 40 | 39 (4) | - |
|  | 30XГCH2A (30XГCHA) | 900 | - | Oil | 260 | Air or oil | 1375 (140) | 1620 (165) | 9 | 45 | 59 (6) | - |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Chrome-manganese-nickel and chrome-manganese-nickel with titanium, molybdenum and boron | 15XГH2TA (15XГHTA) | 960 air | 840 | Oil | 180 | Air or oil | 735 (75) | 930 (95) | 11 | 55 | 98 (10) | 15 |
|  | 20XГHP | 930-950 air | 780-830 | Oil | 200 | Air or oil | 1080 (110) | 1270 (130) | 10 | 50 | 88 (9) | 15 |
|  | 20XГHTP | 850 | - | Oil | 200 | Oil | 980 (100) | 1180 (120) | 9 | 50 | 78 (8) | 15 |
|  | 14XГH | 870 | - | Oil | 150-180 | Air | 835 (85) | 1080 (110) | 8 | - | 78 (8) | - |
|  | 19XГH | 870 | - | Oil | 150-180 | Air | 930 (95) | 1180-1520 (120-155) | 7 | - | 69 (7) | - |
|  | 38XГH | 850 | - | Oil | 570 | Water or oil | 685 (70) | 780 (80) | 12 | 45 | 98 (10) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Chrome-manganese-nickel and chrome-manganese-nickel with titanium, molybdenum and boron | 20XГHM | 860 | _ | Oil | 150-180 | Air | 930 (95) | 1180-1570 (120-160) | 7 | - | 59 (6) | - |
|  | 40XГHM | 840 | — | Oil | 560-620 | Air | 835 (85) | 980 (100) | 12 | - | 88 (9) | 25 |
|  | 25XГHMT | 860 | — | Oil | 190 | Air | 1080 (110) | 1180 (120) | 10 | 40 | 49 (5) | 25 |
| Chrome- nickel-molybdenum | 20XH2M (20XHM) | 860 | 780 | Oil | 200 | Water or oil | 685 (70) | 880 (90) | 11 | 50 | 78 (8) | 15 |
|  | 30XH2MA (30XHMA) | 860 | - | Oil | 530 | air | 785 (80) | 980 (100) | 10 | 45 | 78 (8) | 15 |
|  | 38X2H2MA (38XHMA) | 870 | _ | Oil | 580 | Air or oil | 930 (95) | 1080 (110) | 12 | 50 | 78 (8) | 25 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalization | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |
| Chrome – nickel-molybdenum | 40XH2MA (40XHMA) | 850 | - | Oil | 620 | Water or oil | 1) 930 (95) 2) 835 (85) | 1080 (110) 980 (100) | 12 12 | 50 55 | 78 (8) 98 (10) | 25 25 |
|  | 40X2H2MA (40X1HBA) | 870 | - | Oil | 600 | Water or oil | 930 (95) | 1080 (110) | 10 | 45 | 78 (8) | 25 |
|  | 38XH3MA | 850 | - | Oil | 590 | Air | 980 (100) | 1080 (110) | 12 | 50 | 78 (8) | 25 |
|  | 18X2H4MA (18X2H4BA) | 950 | 860 | Air | 200 | Air or oil | 835 (85) | 1130 (115) | 12 | 50 | 98 (10) | 15 |
|  |  | 950 Air | 860 | Oil | 550 | Air or oil | 2) 785 (80) | 1030 (105) | 12 | 50 | 118 (12) | 15 |

Continuation of table 6

| Group of steel | Grade of steel | Heat treatment | Yield point, (T’ N/мм² (kgf/mm²) | Ultimate strength, (B’ N/мм² (Kgf/mm²) | Relative elongation (5, % | Relative reduction of area (, % | Impact strength KCU, | Cross section al dimension of blank for heat treatment (diameter of round or side of square) , mm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Hardening | Tempering |  |  |  |  |  |  |
|  |  | Temperature (C | Cooling medium | Temperature (C | Cooling medium |  |  |  |  |  |  |
|  |  | 1st hardening or normalizing | 2nd hardening |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | Not less than |  |
| Chrome – nickel-molybdenum | 25X2H4MA (25X2H4BA) | 850 | - | Oil | 560 | oil | 930 (95) | 1080 (110) | 11 | 45 | 88 (9) | 25 |
| Chrome-nickel-molybdenum-silicon and chrome-silicon-nickel | 30XH2MФA | 860 | - | Oil | 680 | Air | 785 (80) | 880 (90) | 10 | 40 | 88 (9) | 25 |
|  | 36X2H2MФA (36XH1MФA) | 850 | - | Oil | 600 | Air | 1080 (110) | 1180 (120) | 12 | 50 | 78 (8) | 25 |
|  | 38XH3MФA | 850 | - | Oil | 600 | Air | 1080 (110) | 1180 (120) | 12 | 50 | 78 (8) | 25 |
|  | 45XH2MФA (45XHMФA) | 860 | - | Oil | 460 | Oil | 1) 1275 (130) 2) 1325 (135) | 1420 (145) 1470 (150) | 7 7 | 35 35 | 39 (4) 39 (4) | - - |
|  | 20XH4ФA | 850 | - | Oil | 630 | Water | 685 (70) | 880 (90) | 12 | 50 | 98 (10) | 25 |